## Slide 1
Photoluminescence Mapping of Vanadium Defects in SiC for Quantum Technology Applications
Zhujing Xu and Tongcang Li
SURF 2024
Daniel Choi
Mentors:
Dr. Lijun Ma
Dr. Anouar Rahmouni
Dr. Oliver Slattery

## Slide 2: Background
Quantum Key Distribution
Distributed Quantum Computing
Distributed Sensing
Blind Quantum Computing
Quantum Network
Idea: Photon-mediated entanglement distribution
|01>
|10>
Alice
Bob
Challenge:
G. Wolfowicz et al., Nat Rev Mater 6 (2021)
No-cloning
Theorem
+
Notes: - Blind quantum computing where a client can securely perform quantum computation on any untrusted device without disclosing information about computation being performed to the server.
-

## Slide 3
Node B
Repeater
Quantum repeater
Hong-Ou-Mandel effect
Entanglement Swapping
Node A
Simultaneity: need quantum memory
Indistinguishability: need reliable single photon source
V defects in SiC
Node C

## Slide 4: Advantages of SiC
G. Wolfowicz et al., Sci. Adv. (2020)
Power Electronics Application Overview, ELE Times Bureau
G. Wolfowicz et al., Nat Rev Mater 6 (2021)
Readout
Initialization
Control
Nuclear Spin Registers
~250 polytypes
Mature growth/fabrication techniques
Telecom Emission
ES1
ES
GS
ES2
GS1
GS2
B > 0
ES1
ES
GS
ES2
GS1
GS2
MW
Notes: Although the transitions are spin conserving to the leading order, the spin orbit interaction and hyperfine interaction can cause weak mixing of the spins in excited state, allowing for spin-flip transitions to initialize the state.

## Slide 5: Motivation
Given a sample of defects in SiC, can we verify that they have properties suitable for quantum network nodes?
  Emission spectrum
  Coherence time
  Single-photon emission
  High-fidelity control
Work | Wolfowicz et al. | Ahn et al. | NIST
Source | Norstel | Coherent | CMU (4H) Coherent (6H)
Implantation Energy | 190 keV | 190 keV | 500 keV 190 keV
Concentration | ~1e8/cm2 | ~7e15/cm2 | ~1e13/cm2 ~1e8/cm2
Annealing | 1400°C | None | 1000°C
Sample Comparison
Practical implementation of quantum network nodes with SiC defects requires robust characterization methods and procedures.
Variation in samples.
  Different manufacturing methods.
  Even with the same manufacturing method, some variance is inevitable.
Investigation of other polytypes.
  ~250 SiC Polytypes
  Every polytype has different properties
Notes: Although the transitions are spin conserving to the leading order, the spin orbit interaction and hyperfine interaction can cause weak mixing of the spins in excited state, allowing for spin-flip transitions to initialize the state.

## Slide 6: Confocal Microscope
UV
365nm
SPD
Swabian
Time Tagger
Piezo Controller
3-Axis Flexure Stage
V-SiC Sample
Nikon Objective
100x
Python
Dichroic
Tunable
Filter
Aspherical
Lens
Mirror
Mirror
20μm
Notes: Although the transitions are spin conserving to the leading order, the spin orbit interaction and hyperfine interaction can cause weak mixing of the spins in excited state, allowing for spin-flip transitions to initialize the state.

## Slide 7: Spectroscopy
V4+ 6H-SiC Spectroscopy α Site
J. Ahn et al., arXiv:2405.16303 (2024)
295 K
V4+ 6H-SiC Spectroscopy | 
Tunable Filter | Santec OTF-980
Detector | SNSPD
Range | 1304-1316 nm
Center λ Step-size | 0.1 nm
Linewidth (Δλ) | 1 nm
Integration time | 20 s
Despite significant doppler broadening, a peak was found around 1308.5 nm, consistent with other studies.
Notes: Although the transitions are spin conserving to the leading order, the spin orbit interaction and hyperfine interaction can cause weak mixing of the spins in excited state, allowing for spin-flip transitions to initialize the state.

## Slide 8: Spatial Mapping
V4+ 4H-SiC Non-resonant PL Mapping
4H-SiC Sample on a Mount
V4+ H-SiC PL Mapping | 
Stage | Thorlabs MAX311D
Controller | Thorlabs KPZ101
Detector | InGaAs/InP SPD
Area | 20μm x 20μm
Increment | 1.05μm (3.94V)
Integration time | 5 s
Higher concentration was found at the centerline (Y=0) as expected based on implantation method.
While a certain degree of repeatability was achieved, higher resolution is required for a more accurate mapping. Future improvement:
  Closed-loop system to avoid hysteresis.
  Cryogenic condition to remove thermal noise and doppler broadening.
Notes: Although the transitions are spin conserving to the leading order, the spin orbit interaction and hyperfine interaction can cause weak mixing of the spins in excited state, allowing for spin-flip transitions to initialize the state.

## Slide 9: Future Work
Cryogenic condition
Spectroscopy of other polytypes and sites
J. Ahn et al., arXiv:2405.16303 (2024)
Spatial PL mapping at resonant frequencies
G. Wolfowicz et al., Sic. Adv. 6 (2020)
P. Cilibrizzi et al., Nat Commun 14 (2023)
Single-photon emission
Integration in photonic crystal cavities
Relaxation and coherence time
Doping concentration
  Charge stability
Isotopic composition
  Narrow inhomogeneous distribution
Strain tuning
  Coherence time
G. Calusine et al., Phys. Rev. Applied 6 (2016)
Coherent spin control
R. Nagy et al., Nat Commun 14 (2019)
Montana Instruments
Experimental Demonstration
Notes: Although the transitions are spin conserving to the leading order, the spin orbit interaction and hyperfine interaction can cause weak mixing of the spins in excited state, allowing for spin-flip transitions to initialize the state.

## Slide 10: Conclusion
Set up the experiment to characterize V4+ defects in SiC
  Spectroscopy was consistent with other studies.
  PL Mapping confirmed expected doping concetration gradient.
  A certain degree of repeatability was achieved.
This work will
enable characterization of V4+ defects in other polytypes
enable further investigation to validate the potential of V4+ SiC for quantum application.
Notes: Although the transitions are spin conserving to the leading order, the spin orbit interaction and hyperfine interaction can cause weak mixing of the spins in excited state, allowing for spin-flip transitions to initialize the state.